Clayey raw materials for archaeological and traditional ceramics and firing processes

Alberto De Bonis

12 ore – 3 CFU

Short Program:

- Clayey raw materials for archaeological and traditional ceramics from the Campania Region of Italy: Origin, composition, and technological features – 4 hours

• 	Firing processes and technological features of the ceramic products – 4 hours

• 	Archaeometric studies of ceramics: sourcing raw materials and production techniques – 4 hours

Suggested Background: Mineralogy and petrography